# SECTION 02795 – POROUS PAVEMENTS

PART 1 – GENERAL

1.1 	General Provisions

A.  The Conditions of the Contract and all Sections of Division 1 are hereby made a part of this Section.

1.2 	Description of Work

A.  Work Included:

1.   Provide and install sandy gravel road base as shown on drawings, to provide adequate support for project design loads.  See 2.2 Materials.

2.   Provide EZ Roll Grassroad Paver Paving System products including EZ Roll Grassroad Paver units, and installation per the manufacturer's instructions furnished under this section.

3.   Provide and install specified topsoil to fill the EZ Roll Grassroad Paver units, when needed.

4.   Provide and install grass by using method per plans.

B.  Related Work:

1.   Subgrade preparation under Section 02200 Earthwork.

2.   Subsurface drainage materials - Section 02720 Storm Drainage, when needed

3.   Irrigation installation - Section 02810 Irrigation, when needed.

1.3 	Quality Assurance

A.  Follow Section 01330 requirements.

B.  Installation:  Performed only by skilled workpeople with satisfactory record of performance on landscaping or paving projects of comparable size and quality.

1.4 	Delivery, Storage, and Handling

A.  Protect EZ Roll Grassroad Paver units from damage during delivery and store under tarp to protect from sunlight, when time from delivery to installation exceeds one week.

1.5 	Project Conditions

- Review installation procedures and coordinate EZ Roll Grassroad Paver work with other work affected.  Generally, EZ Roll Grassroad Paver is installed at the same time as project grass installation, nearly the last site construction activity.

- All hard surface paving adjacent to EZ Roll Grassroad Paver areas, including concrete walks and asphalt paving should be completed prior to installation of EZ Roll Grassroad Paver.

- Slopes for EZ Roll Grassroad Paver surfaces can vary from flat to 10%+, depending upon vehicle types to use the surface.  Please note that fire lanes, or other emergency vehicles, will generally require a slope that is 10% or less in accordance with IFC D103.2.  If there are any questions regarding existing slopes on this project, please contact the Landscape Architect or Civil Engineer.

- Recommendation: 0% - 5% no stakes, 6% - 10% stakes, (reference staking detail), 10%+ deep anchors (landscape architect or civil engineer to provide detail)

D.  Cold weather:

1.   Do not use frozen materials or materials mixed or coated with ice or frost.

2.  Do not build 	on frozen work or wet, saturated or muddy subgrade.

E.  Protect partially completed paving against damage from other construction traffic when work is in progress, and until grass root system has matured (about 3 to 4 weeks).  Any barricades constructed must still be accessible by emergency and fire equipment during and after installation.

F.  Protect adjacent work from damage during EZ Roll Grassroad Paver installation.

PART 2 – PRODUCTS

2.1 Availability

A.  Manufacturer: NDS, Inc., 851 North Harvard Avenue, PO Box 339, Lindsay, California 93247. Toll Free (800) 726-1994. Toll Free Fax (800) 726-1998. Phone (559) 562-9888. Fax (559) 562-4488.  Website: www.ndspro.com.  E-Mail nds@ndspro.com.

2.2 Materials

- Base Course - Example: Sandy gravel material from local sources commonly used for road base construction, passing the following sieve analysis.

% Passing	 	Sieve Size

100				3/4"

85				3/8"

60		 		#4

30		 		#40

< 3				#200

1.  Sources of the material may include "pit run" or "crusher run.”  Crusher run material will typically require sand be added (33% by volume) to ensure long term porosity.  Should local sources not be available an alternative mixture can be created by mixing 2/3 crushed stone (0.75” dia.) with 1/3 sand as available.

2.  Alternative materials such as a washed or clean stone (0.75” Diameter Typical) stone may be used; however a soil separator must be installed above stone base and below growing medium.

B.   EZ Roll Grassroad Paver Grass Paving Units: Injection-molded, linked and nested honeycomb cell, rolled grass paver structure (24"x24"x1" high, 4.0 ft2 each) with Seventy-two 2-1/4-inch hexagonal cells in nested honeycomb form, with integrated cross-links to allow for rollout installation allowing maximum grass root penetration and development. Top Surface of Hexagonal Cell Wall is smooth, without notches or grooves. Bottom Surface Open Area is greater than 80 percent or 478 square inches per paver section. The plastic shall be 100% recycled Polyolefin with UV inhibitors. Loading capability is equal to 57,888 PSF when empty and 500,000 PSF when filled, over an appropriate depth of road base.  Standard color is black.  Unit weight = 2.31 lbs.  Units may also be shipped in pre-assembled into rolls that vary from 3.96 feet x 24 feet (95.1sf) to 152’L x 3.96’W (601.6 sf), (Measurements at 70 degrees). Panels are assembled with lateral snap locks.

C.  Soil:  Obtain specified topsoil to fill the 1-inch (25 mm) high cells and spaces between the cells when seeding.

PART 3 – EXECUTION

3.1 Inspection

A.  Examine sub-grade and base course installed conditions.  Do not start EZ Roll Grassroad Paver installation until unsatisfactory conditions are corrected.  Check for improperly compacted trenches, debris, and improper gradients.

B.  Installation constitutes acceptance of existing conditions and responsibility for satisfactory performance.  If existing conditions are found unsatisfactory, contact Quality Control Manager for resolution.

3.2 Preparation

A.  Place base course material over prepared sub base to grades shown on plans, in lifts not to exceed 6” (150 mm), compacting each lift separately to 95% Modified Proctor.  Leave minimum (1”) 25 mm for EZ Roll Grassroad Paver unit and soil, fill to Final Grade.

3.3 Installation of EZ Roll Grassroad Paver Units

A.  Install the EZ Roll Grassroad Paver units by placing units with rings facing up and connect the lateral snap locks provided to maintain proper spacing and interlock the units. Units can be easily shaped with hand pruner’s.  Maintain 1” clearance to any pre-installed object or surface structure. Units placed on curves and slopes shall be anchored to the base course, using soil nails with fender washer (or alternate), as required to secure units in place.  Tops of cells shall be between 0.25" to 0.5" below the surface of adjacent hard-surface pavements.

B.  Install specified topsoil in cells as they are laid in sections by dump truck or other equipment, or from buckets mounted on tractors, soil should be added to the cells from an area already filled with soil.  Soil should be spread to fill each cell to the top surface.

3.4 Installation of Grass – See Section 02931 Hydroseed and 02937 Soil Preparation (other methods of installing grass may be acceptable such as sod)

A. 	Hydroseeding/hydro-mulching - A combination of water, seed and fertilizer are homogeneously mixed in a purpose-built, truck-mounted tank. The seed mixture is sprayed onto the site at rates shown in specification section 02931 Hydroseed.  Coverage must be uniform and complete.  Following germination of the seed, areas lacking germination larger than 8" x 8" must be reseeded immediately. Seeded areas must be fertilized and kept moist during development of the turf plants.

B. 	A light “dusting” of imported topsoil mix, not to exceed 1/2” (25 mm) can be placed above the rings and seed mix to aid germination rates.  Seeded areas must be fertilized and kept moist during development of the turf plants.

3.5 Protection

A.  	Seeded areas must be protected from any traffic, other than emergency vehicles, for a period of 4 to 6 weeks, or until the grass is mature to handle traffic.

3.6 Cleaning

A.  	Remove and replace segments of EZ Roll Grassroad Paver units where three or more adjacent cells are broken or damaged, reinstalling as specified, so no evidence of replacement is apparent.

B.  	Perform cleaning during the installation of work and upon completion of the work.  Remove all excess materials, debris, and equipment from site.  Repair any damage to adjacent materials and surfaces resulting from installation of this work.

END OF SECTION 02795